	DJN Part No. DR/C1025

	Style
	Double open ended cylinder
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	Height
	660 mm
	

	Outside diameter
	352 mm
	

	Inside diameter
	241 mm
	

	Gasket inside diameter
	255 mm
	

	Pleat number
	350
	

	Pleat depth/Area
	50 mm/23m2
	

	Equivalent to 
Donaldson Part No
	262 5025
	

	Pleat spacing
	Pleatlock – ensures uniform pleat spacing on both inside and outside diameters for maximum life with minimum airflow restriction. 

	Filter media
	A water-resistant blend of cellulose and synthetic fibres, corrugated to ensure uniform pleat spacing and maximum dust holding capacity. 

	Inner and outer sleeve
	Galvanised expanded steel supports the media pack and protects the media from damage.

	Pleat tip bonding
	The pleats are securely fixed to the outer sleeve by beads of hot melt adhesive to maintain even pleat spacing and prevent movement during pulsing.

	End caps
	Galvanised steel for lifetime rust resistance. 

	Gasket
	A moulded triangular section, permanently bonded to the end cap ensures an airtight seal.  

	Pleat/end cap bonding
	Chemical cure polyurethane system eliminates air by-pass and provides maximum structural strength.

	Filter class
	F7

	Operating temperature
	-29ºC to +80ºC


