RS RUBBER CORPORATION		973-777-2200  FAX 973-777-7175
General Application Gasketing
	 KLINGERSIL® C-4401
	 

	• Synthetic Fiber
• Nitrile Binder
• Excellent Sealability
• Excellent Chemical Resistance
• Good Creep Relaxation
• General Purpose Sheet
Typical values refer to 1/16" material 
unless otherwise specified. 
See graphs for temperature & pressure limits
	

	Creep Relaxation ASTM F38B (1/32")
	20%

	Sealability ASTM F37A (1/32") 
	<0.25 ml/hr

	Gas Permeability DIN 3535/6 
	<0.5 ml/min

	Compressibility ASTM F36J
	7%

	Recovery ASTM F36J 
	50% minimum

	Klinger Hot Compression Test 
	 

	Thickness Decrease 73°F (23°C) 
	10.5% initial

	Thickness Decrease 572°F (300°C)
	17% additional

	Weight Increase 
	 

	ASTM F146 after immersion in Fuel B
5h/73°F (23°C) 
	
10% maximum

	Thickness Increase 
ASTM F146 after immersion in 
	 

	ASTM Oil 1, 5h/300°F (149°C) 
	0-5%

	ASTM Oil IRM903, 5h/300°F (149°C)
	0-5%

	ASTM Fuel A, 5h/73°F (23°C)
	0-5%

	ASTM Fuel B, 5h/73°F (23°C) 
	0-7%

	Dielectric Strength 
	 

	ASTM D149-95a
	14 kV/mm

	ASTM F104 Line Call Out
	F712121B3E12K6M5

	Leachable Chloride Content
FSA Method (Typical)
	
100 ppm

	Density ASTM F1315
	112 lb/ft3 (1.8 g/cc)

	Color (Top/Bottom)
	Green

	Pressure & Temperature Graphs Material Thickness: 1/16" 





C4401 charts see below
Liquids   C4401
[image: http://thermosealinc.com/THERMO_CHARTS/C-4401.jpg]
 

	Gases & Steam C4401
[image: http://thermosealinc.com/THERMO_CHARTS/C-4401_2.jpg]
 


About Pressure and Temperature Graphs
The pressure/temperature graphs shown are the most current method of determining the suitability of a gasket material in a known environment. Use the pressure and temperature graphs to select the most suitable material for your application.
	 
	1.
	In area one, the gasket material is suitable using common installation practices subject to chemical compatibility.

	 
	2.
	In area two, appropriate measures are necessary for installation of the gasket to ensure maximum performance. Please call or refer to the KLINGER® expert software system for assistance.

	 
	3.
	In area three, do not install gaskets in these applications without first referring to the KLINGER® expert software system 


[bookmark: _GoBack]These graphs were developed from testing Klinger materials. Do not use them for competitors' materials since non-asbestos gasketing materials do not have service equivalents.

Use: The limitations of use, as shown in the graphs, are for guidance only, and are based on 1/16" thick material. The limitations of use decrease significantly as gasket thickness increases. Do not use a thicker gasket material or "double gaskets" to solve a gasket problem without first consulting the manufacturer. The ability of a gasket material to make and maintain a seal depends not only on the quality of the gasket material, but also on medium being sealed, the flange design, the amount of pressure applied to the gasket by the bolts and how the gasket is assembled into the flanges and tightened
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