	DJN Part No. DRC1002

	Style
	Single open ended cylinder
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	Height
	660 mm
	

	Outside diameter
	324 mm
	

	Inside diameter
	212 mm
	

	Gasket inside diameter
	255 mm
	

	Pleat number
	320
	

	Pleat depth
	50 mm
	

	Filtration area
	21 m²
	

	Pleat spacing
	Pleatlock – ensures uniform pleat spacing on both inside and outside diameters for maximum life with minimum airflow restriction. 

	Filter media
	A water-resistant blend of cellulose and synthetic fibres, corrugated to ensure uniform pleat spacing and maximum dust holding capacity. 

	Inner and outer sleeve
	Galvanised expanded steel supports the media pack and protects the media from damage.

	Pleat tip bonding
	The pleats are securely fixed to the outer sleeve by beads of hot melt adhesive to maintain even pleat spacing and prevent movement during pulsing.

	End caps
	Galvanised steel for lifetime rust resistance. 

Closed cap with 13mm bolt hole

	Gasket
	A moulded triangular section, permanently bonded to the end cap ensures an airtight seal.  

	Pleat/end cap bonding
	Chemical cure polyurethane system eliminates air by-pass and provides maximum structural strength.

	Filter class
	F7

	Operating temperature
	-29ºC to +80ºC


