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	Product Code:
	Form P121-10N


	Description:
	Scrub Test Panel


	Material:
	Black Plastic – Vinyl Chloride / Acetate Copolymer

	Surface:
	Smooth matte – Plasticizer Free


	Density:
	1.28 – 1.34 g/cc


	Dimensions:
	165 x 432 mm (6.5 x 17 in)


	Thickness:
	0.25 mm (0.010 in)


	Visual:
	Free of visual anomalies


	Packaging:
	Packed 100 sheets per box and 5 boxes per case

	




If the contents of this box are RED, this is a controlled copy of this document.              





Title:  Specification Sheet	P121-10N           Document No.: P121 10N 01


				     


Generated By: JPeters	         Dated:  2012-03-14                     Page:     1 of 1 


      


Approved By: Dan Schaeffer      Dated:   2012-03-14               Version:     0.0.0








Revision History:





Rev No.�
Date�
Reason/Content�
�
�
�
�
�
�
�
�
�
�
�
�
�
�
�
�
�
�
�
�
�









This document is the property of The Leneta Company, all rights reserved.  Reproduction, replication or storage in any medium by third parties is forbidden except with written authority.

